Kiln Wash – Continental Clay Company

Mixing Instructions:

- Add 1 lb. Kiln Wash to approx 12 oz. water

(start slow, adding powder to water and add more water as needed)

- You are looking for a consistency similar to thick cream

- Stir the container frequently while using to avoid settling

Shelf Preparation:

- Scrape off  loose debris* and remove any dust (vacuum)

- Wipe shelves with warm water to reduce absorbency

- Apply the kiln wash to one side of the shelf (brush or roller)

- Use three thin coats of kiln wash instead of one thick coat

- Allow kiln wash to dry slightly in between coats

- Change the direction of each coat

- While the shelf is wet it will appear as though there is no kiln wash, it will show as it dries and after the shelf has been fired

- Remove any drippings from the edges of the shelves to avoid flaking onto lower shelf ware

- Allow kiln wash to dry thoroughly before using shelf (time will vary with humidity and drying conditions, but expect at least 1-2 hours)

- A freshly kiln washed shelf does not need to be pre-fired or cured

- A kiln washed shelf lasts 2-10 firings depending on conditions

Note:  Kiln wash can also be applied to the floor (bottom) of the kiln.  Do not splash kiln wash onto elements or the kiln walls.

* shelf cleaning block

Continental Clay Company

1101 Stinson Blvd NE

Minneapolis, MN   55413

(800) 432-CLAY

www.continentalclay.com