POTTERY PLASTER K-60   CHPLK60   MIXING INSTRUCTIONS

Ideal for molds, bats, wedging surfaces, etc.

Use 70 parts Water per 100 parts Plaster

=

1 ½ lbs. plaster to 1 lb. water

Note:	Warm water temperature will cause plaster to set up faster than cold water. Use water that is fit to drink.

	Fill mixing container with correct amount of water

needed to mix dry plaster (70/100 ratio)

	Add plaster to water (not water to plaster) mounding in the center of the

Water. (sift plaster into water, soak until all particles are wet).

	Mix thoroughly. Mix the slurry to a creamy state to avoid settling.

When pouring, maintain a constant rate, keeping the lip of the bucket as close to the mold as possible.

Drying

(Ideal conditions, but not mandatory)

- So that a mold's physical properties can develop to the maximum level, the mold should be dried as quickly, thoroughly and safely as possible.

- Drying is the evaporation of "free" water from the mold which can be either a natural or forced air process.

- When the center of the piece reaches the temperature of the air surrounding it, drying is complete.

To prevent calcination (soft, powdery surfaces), drying temperatures generally should not exceed 120°F. Drying times can be reduced by increasing air speed over plaster molds. The following conditions are present in the best drying rooms:

- Rapid, consistent air circulation with no 'dead spots'

- A consistent temperature throughout the area

- An air transfer system that replaces exhausted, moist air with dry air

Continental Clay Co  ·  1101 Stinson Blvd NE  · Minneapolis, MN  55413  (612) 331-9332  (800) 432-CLAY

www.continentalclay.com